## Slide 1
Additives for Coatings
J&C Global Tech. Co., Ltd.

## Slide 2
CONTENTS
Defoamers
Dispersant
Rheology modifiers
Preservative
Wetting agent
UV-Monomers

## Slide 3
1-2. Classification of Defoamer
Type | Composition | Feature | Application | Product Name
Mineral Oil type | Mainly mineral oil | Construction paint, Finishing Materials, Latex, etc, wide usage | Matt, Semi-gloss, emulsion, Latex, Plastic, etc | UNIFLOW-NXZ, UNIFLOW-NDW, UNIFLOW DF-311, UNIFLOW-313K
Modified silicon type | Strong lypophilic silicon oil emulsion | No gloss loss No color identification | Clear Paint, Less PVC contents paint for wood, Gloss paint, etc | UNIFLOW DF-399, UNIFLOW DF-300, UNIFLOW-DEFOAMER 1311
Oil based type | Modified fluor Poly-siloxane | Very strong defoaming property Excellent performance at paint formular without aromatic solvent | Acryl, Alkyd paint, Stoving paint, Oil-based type paint | UNIFLOW DAPPO SERIES, UNIFLOW DF-504
Silica silicon type | Adsorption with SiO2 and Silicon | Stable to Crater on film surface Wide usage | Latex, Emulsion, Aquous paint, Ink , Adhesives, Finishing materials, Futty, etc | UNIFLOW 8034L UNIFLOW 777S UNIFLOW 483
None silicone type | Special Polymer (Amide, Polyether, Powder type, etc) | Good anti-foaming performance Improved dispersible in water Control film trouble like crater, etc Good gloss improve property | Aquous resin, ceramics, Aquous paint | UNIFLOW DF-800, DF-180, DF-184, UNIFLOW OSI, DF-901, DF-891

## Slide 4
1-3. Product list of defoamer
Type | Usage | Product Name | Feature | Counter type
Constructional Paint | Flat paint | UNIFLOW-DEFOAMER 313K | - Excellent foam breaking and anti-foaming ability - Good for foam-prone conditions such as roller coating - Water based semi-gloss emulsion paint. Exterior finishing material, | DAPRO 7010, ADEKANATE B556
 |  | UNIFLOW NXZ | General purpose defoamer for various fields. Synthetic latex, emulsion paint, Adhesive, construction putty | 
 |  | UNIFLOW NDW | General purpose defoamer for various fields. Latex, acryl acetate, EVA, acryl emulsion, construction putty, adhesive. | 
 |  | UNIFLOW DF-101 | Excellent foam breaking and anti-foaming ability for water based emulsion - FLAT, SEMI-GLOSS emulsion paint. Exterior finishing material. | 
 | Semi-gloss paint | UNIFLOW DF-8034L | - General-purpose defoamer which has good anti-foaming ability Good coating film without crater, gloss loss - Latex, Water based paint, emulsion, ink, adhesive, Finishing materials | BYK-034
 |  | UNIFLOW DF-800 | Excellent foam breaking and anti-foaming ability at any system Good at foam on surface and micro foam in liquid Suitable Zero VOC | BYK-012, 014
 | Hi-gloss paint | UNIFLOW-DEFOAMER 399 | - Excellent performance in anti foaming Less gloss loss and less craters - Water based paint, ink, emulsion and adhesive | BYK-024, FOAMAX 825, COGNIS 1620
 |  | UNIFLOW-DEFOAMER 1311 | - Product with improved the performance of SN-DEFOAMER 399 Less gloss loss and less craters, excellent foam breaking and long-lasting anti-foaming ability. - Water based paint, ink, emulsion and adhesive. Paint for low pollution | BYK-024, COGNIS 1293
 | Elastomeric Paint | UNIFLOW DF-400 | - Silicon type defoamer for high viscosity No degradation in gloss and micro-foam - Silicon elastic paint. High viscosity paint | ADEKA B187
Powder | Powder | UNIFLOW-DEFOAMER 14HP | - Pre-mix type powder defoamer Excellent foam breaking performance for quality improvement of products For various type of powder | 
Automotive and Industrial | Primer | UNIFLOW 122NS | Excellent anti-forming performance without crater Water based paint, ink | 
 | Electrodeposition coat | UNIFLOW DF- 901 | - Good ability to decrease the surface tension, Good wetting and leveling effect. Automotive coatings, water based paint, ink and emulsion, adhesive. | 

## Slide 5
2-2. Classification of Dispersant
Composition
Hydrophobic
Hydrophilic
Neutralization
Sodium salt
Ammonium salt
UNIFLOW-DS 44S
For filler (CaCO3 etc.)
For universal pigments
(TiO2, CaCO3 etc.)
For universal pigments
(TiO2, CaCO3 etc.)
Advantage
・Water resistance
・Wetting for organic pigments
UNIFLOW-DS 5027
UNIFLOW-DS 5029
UNIFLOW-DS 5034
UNIFLOW-DS 5468
Advantage
・ water resistance
・ anti-settling
For filler (CaCO3 etc.)
UNIFLOW-DS 2026S

## Slide 6
2-3. Product list of Dispersant
Application | Product Name | Type | NV | Feature | Counter type
Inorganic Pigment | UNIFLOW-DS 44S | Polycarboxylic acid sodium salt | 43% | - Effective for decreasing viscosity of slurry and dispersing TiO2, CaCO3, inorganic pigment - Very stable to temperature and no effect to increase viscosity - For water soluble | OROTAN 963
 | UNIFLOW-DS 5034 | Polycarboxylic acid sodium salt | 45% | - Excellent dispersing performance for PCC, inorganic pigment - Good quality for storage. - Dispersant for water based | OROTAN 850, COGNIS 5040
 | UNIFLOW-DS 5807 | Polycarboxylic acid | 50% | - Excellent dispersing performance for PCC, inorganic pigment, concrete - Good quality for storage. - Dispersant for water based | 
Give water resistance | UNIFLOW-DS 5027 | Polycarboxylic acid ammonium salt | 20% | - Dispersant for organic and inorganic pigment with excellent water and rust resisting quality - Product with improved the water resisting quality of SN-DISPERSANT 5029 - For water based emulsion, paint | EFKA 4560
 | UNIFLOW-DS 5029 | Polycarboxylic acid ammonium salt | 25% | - Dispersant for organic and inorganic pigment with excellent water and rust resisting quality, - Product with improved the dispersing performance of SN-DISPERSANT 5027 For water based emulsion, paint Good compatibility | ORORTAN 731SD, EFKA 4550, 4570
 | UNIFLOW DS-2029 | Polycarboxylic acid ammonium salt | 30% | - Good water resisting, and rust resisting quality - Effective for inorganic pigment such as TiO2, clay. etc - For water based emulsion paint, waterproof flooring material. | OROTAN 731
 | UNIFLOW-DS 5468 | Polycarboxylic acid ammonium salt | 40% | - Excellent dispersing effect for organic and inorganic pigment - Improve water tolerance and rust resisting quality - For water based emulsion paint, waterproof flooring material | 
 | UNIFLOW DS-201 | Polycarboxylic acid sodium salt | 30% | - Good water resisting, and rust resisting quality - Effective for inorganic pigment such as TiO2, clay. etc - For water based emulsion paint, waterproof flooring material. | OROTAN 731

## Slide 7
2-3. Product list of Dispersant
Application | Product Name | Type | NV | Feature | Counter type
Organic Pigment | UNIFLOW DS-1520 | Polycarboxylic acid | 35% | - Excellent performance for dispersing organic pigment and carbon black - Good water resistance and rust resistance For water based flexography and gravure ink, industrial paint, pigment toner, inkjet ink | TEGO DISPERSE-760W
 | UNIFLOW DS-1040 | Polycarboxylic acid | 40% | - Excellent performance for dispersing TiO2, organic pigment and carbon black Excellent performance of decreasing viscosity, coloring, water resistance and rust resistance. For water based paint, automotive coatings, wood coatings, flexography and gravure ink | BYK-190
Oil-based | UNIFLOW DS-202 | Polycarboxylic acid amine salt | 50% | - Excellent wetting, anti-settling, dispersing performance for oil based paint and ink - For alkyd, acryl, epoxy, chlorinated rubber, polyurethane, vinyl chloride resin | BYK-115
 | UNIFLOW DS-203 | Polyethylene | 100% | - Excellent performance for processing PVC plastisol Very effective for dispersing CaCO3, TiO2, ZnO | BYK-110
 | UNIFLOW DS-365 | Acryl copolymer | 45% | Good dispersing property Hi-gloss, good color acceptance Improve hiding power and transparency Decrease viscosity, Improve leveling Possible to make high solid paint | BYK-163

## Slide 8
3-2. List of HASE rheology modifier
Product Name | Type | VOC | Application | Feature
UNIFLOW-TN 618 | Modified Poly-acryl emulsion | Free | Emulsion paint, water based paint | - Water soluble product for coating color. - Good decay stability. Improve flow and repair property, give good thixotropic performance - NP free type
UNIFLOW-TN 641 |  | Free | Emulsion paint, water based paint, emulsion adhesive, water based ink | - High solid and strong thickening property - Good decay stability. - Good flow and leveling performance, no gloss loss - NP free type

## Slide 9
3-4. List of Urethane Rheology modifier(HEUR)
Product Name | Type | VOC | Application | Feature
UNIFLOW-TN 622N | Urethane modified polyether | Contain | Water based emulsion paint, emulsion adhesive, water based ink | Thickener which has strong thickening and good leveling performance - Good adhesiveness for elastic paint and tile paint - Viscosity and pattern can be controlled using with thixotropic thickener
UNIFLOW TN-1500 |  | Free | Emulsion paint, water based paint, emulsion adhesive, water based ink | Thickener which has strong thickening and good leveling performance - Good adhesiveness for elastic paint and tile paint - Viscosity and pattern can be controlled using with thixotropic thickener
UNIFLOW TN-1002 |  | Free | Emulsion paint, water based paint, emulsion adhesive, water based ink | - Solvent free, eco friendly Zero VOC type - Good flow and leveling performance, no gloss loss Viscosity and pattern can be controlled as its thixotropy property
UNIFLOW TN-1000 |  | Free | Emulsion paint, water based paint, emulsion adhesive, water based ink | - Solvent free, eco friendly Zero VOC type - Good flow and leveling performance, no gloss loss
UNIFLOW TN-1009 |  | Contain | Emulsion paint, water based paint, emulsion adhesive, water based ink | - Good thermo-sensitive and good toning property - Good flow and leveling performance, no gloss loss Viscosity and pattern can be controlled as its thixotropy property.

## Slide 10
3-5.Chart of Urethane Rheology modifier(HEUR)
Thixotropic
Newtonian
ＴＩ
Viscosity
Viscosity propety
大
小
●：Solvent type ○: Solvent free
● UNIFLOW TN-1009
● UNIFLOW TN 622N
○ UNIFLOW TN-1000
○ UNIFLOW TN-1002
○UNIFLOW TN-1500

## Slide 11
4. Product List of Preservative
Product Name | Type | Application | Feature
UNIFLOW CIDE-315 | Hydro alcohol | - Water based color, resin, emulsion paint | - No heavy metals contained - Effective for pH more 8 - Safe sterilizing effect. no bad odor.
UNIFLOW CIDE-200 | Triazine | - Water based color, resin, emulsion paint | - Low toxic preservative without heavy metals - Effective for pH more 8
UNIFLOW CIDE-115 | Hydro alcohol | - Water based color, resin, emulsion paint | - No heavy metals contained - Effective for pH more 8 - Safe sterilizing effect. no bad odor.
UNIFLOW CIDE-135S | CMIT & others | - Water based color, resin, emulsion paint | - Low toxic preservative without heavy metals - Excellent sterilizing performance - Effective for pH 4~7, no bad odor

## Slide 12
5. Product list of wetting agent
Product Name | Type | Application | Feature
UNIFLOW WT-100 | Non-ionic 50% | -Water based paint and ink -Coating | - Provides defect-free defoaming and dynamic wetting benefits in waterborne coatings - Inhibits foam generation in processing and application with added surface tension reduction that improves substrate wetting and appearance.
UNIFLOW WT-110 | Non-ionic 80% | -Water based paint and ink -Coating | - Provides defect-free defoaming and dynamic wetting benefits in waterborne coatings - Inhibits foam generation in processing and application with added surface tension reduction that improves substrate wetting and appearance.
UNIFLOW-WT 366 | Non-ionic 70% | - Water based paint and emulsion | - Non-ionic wetting agent - Excellent wetting property - No coagulation problems
UNIFLOW WT-900 | Non-ionic 100% | - Water based paint, ink, adhesive, UV paint | - Modified silicon surfactant, polyether, water based coatings - Good effect decreasing surface tension, give excellent wetting property
UNIFLOW WT-901 | Non-ionic 100% | Water based paint, ink, Paper coating paint, latex | Good effect decreasing surface tension Improve wetting ability and leveling property or paint and emulsion
UNIFLOW WT-972 | Non-ionic 100% | - Water based paint and ink | - High performance wetting agent for wide range of pH - Low foaming wetting agent - Good wetting, leveling property - No craters, Improve workability and storability
UNIFLOW WT-973 | Non-ionic 100% | - Water based inorganic pigment, paint, ink, adhesive - Emulsion, Latex | - Good effect decreasing surface tension, give excellent wetting property - Protect from discoloration - High performance wetting agent for wide range of pH - Non-silicon type, good recoating ability
UNIFLOW-WT 980 | Non-ionic 100% | Water based paint and ink Paper coating paint, emulsion Latex | Good ability to decrease surface tension Excellent wetting ability and leveling performance. Low foams
UNIFLOW-WT 984 | Non-ionic 100% | Water based paint and ink Paper coating paint, emulsion Latex | Good ability to decrease surface tension Excellent wetting ability and leveling performance. Low foams

## Slide 13
6. UV monomers
Product Name | Description | Func. | Color (GARDNER) | Solid (%) | Viscosity (at 25℃) | Mw | Characteristics
UNIMER 2000 (HDDA) | Hexanediol Diacrylate | 2 | ≤1 | 100 | 5~15 | 226 | Good adhesion Low volatility Fast curing
UNIMER 3000 (TMPTA) | TrimethylolPropane Triacrylate | 3 | ≤1 | 100 | 80~120 | 296 | Good abrasion resistance Low volatility Fast curing
UNIMER 3401 (PETA) | Pentaerythritol Triacrylate | 3~4 | ≤1 | 100 | <1,000 | 298 | Very fast cure response when exposed to Ultraviolet or electron beam.
UNIMER 4612 (DPHA) | Dipentaerythritol Hexaacrylate | 5~6 | ≤2 | 100 | 5,000~9,000 | 540 | High density of Acrylate make high surface-hardness and high curing velocity, low odor, low skin irritancy
UNIMER 5600 (DPPA) | Dipentaerythritol Pentaacrylate | 5~6 | ≤1 | 100 | 5,000~9,000 | 524 | High density of Acrylate make high surface-hardness and high curing velocity, low odor, low skin irritancy

## Slide 14
6. UV functional acrylate oligomer
Product Name | NV | Viscosity (cPs, 25℃) | Func. | Characteristics
UNIMER 8205H | 65± 2 (HDDA) | (25℃) 1,400 | 2 | Good flexibility , good adhesive performance, Non-yellowing, High solvent resistance
UNIMER 8205 | 100 | (40℃) 13,600 | 2 | Good flexibility , good adhesive performance, Non-yellowing, High solvent resistance
UNIMER 8300F | 70 ± 2 | 300 | 3 | Low viscosity & flexibility, Outstanding toughness & stain resistance, Non-yellowing
UNIMER 8300 | 100 | 8,000 | 3 | Good flexibility , toughness and exterior durability Very low viscosity coatings
UNIMER 8300T | 100 | 70,000 | 2 | Good abrasion resistance, Good flexibility & heat resistance, Exterior durability, Excellent toughness, Adhesion to various substrate, Non-yellowing
UNIMER 8856T | 80 ± 2 | 780 | 6 | High hardness & scratch resistance, High solvent resistance, High gloss, Extremely fast cure speed, Non-yellowing
UNIMER 8859T | 100 | 20,000 | 6 | High hardness & scratch resistance, High solvent resistance, High gloss, Extremely fast cure speed, , Non-yellowing
UNIMER 8960T | 75 ± 2 | 2,500 | 9 | High hardness & excellent abrasion resistance, High scratch & solvent resistance, Good toughness & gloss, Non-yellowing
UNIMER 8906T | 100 | 50,000 | 10 | Very high hardness & excellent scratch resistance, Excellent chemical resistance, Extremely fast cure speed, Non-yellowing

## Slide 15
Thank you
J&C Global Tech. Co., Ltd.
101-911 CHUNUI TECHNOPARK, CHUNUI-DONG, WONMI-GU, BUCHEON-CITY, KYUNGGI-DO, 420-857, SOUTH KOREA
TEL: +82-32-613-4211 FAX: +82-32-613-4213
E-MAIL: juno4122@jncgt.com